Chapter 5 - Static Failure Theories

Rule of Thumb:

-Ductile, isotropic materials in static tensile loading are limited by their shear strengths…

→ Although, sometimes ductile materials can act like brittle materials.

-...Brittle materials are limited by their tensile strengths…

With Regards to Fracturing:

-Only ductile materials may yield significantly before fracturing.

→ Note that if cracks are present in a ductile material, it can suddenly fracture at nominal stress levels well below the yield strength, even under static loads.

-Brittle materials proceed to fracture without significant shape change.

Difference between Static and Dynamic Loads

-Static loads are applied slowly and remain constant over time.

-Dynamic loads are either suddenly applied (impact loads) or repeatedly varied with time (fatigue loads), or both.

-There are also four classes in which components fail due to motion.

5.1 Failure of Ductile Materials Under Static Loading

Historically, several theories have been formulated to explain this failure

-Maximum normal-stress theory, maximum normal-strain theory, total strain-energy theory, distortion-energy (von Mises-Hencky) theory, and maximum shear-stress theory.

-The von Mises-Hencky theory is the most accurate with experimental data.

5.1.1 The von Mises-Hencky or Distortion-Energy Theory

-The microscopic yielding mechanism is now understood to be due to relative sliding of the material’s atoms within their lattice structure.

-This sliding is caused by shear stress and is accompanied by distortion of the shape of the part.

-The energy stored in the part from this distortion is an indicator of the magnitude of the shear stress present.

5.1.1.1 Total Strain Energy

The strain energy U in a unit volume (strain energy density) associated with any stress is the area under the stress-strain curve up to the point of the applied stress for a unidirectional stress state.

→ Assuming that the stress-strain curve is essentially linear up to the yield point, then we can express the total strain energy in a unit volume at any point in that range as

U=12σ*ε	{for 1D stress state, units J*m3kg}

U=12*σ1*ε1+σ2*ε2+σ3*ε3	{3D stress state}

σ1, σ2, and σ3 Principal stresses

ε1, ε2, and ε3 Principal strains

The above 3D equation uses the principal stresses and principal strains that act on planes of zero shear stresses.

Principal strains with respect to the principal stresses:

ε1=1E*(σ1-ν*σ2-ν*σ3)

ε2=1E*(σ2-ν*σ1-ν*σ3)

ε3=1E*(σ3-ν*σ1-ν*σ2)

ν = Poisson's ratio

3D Strain Energy density with respect to only the principal stresses

U=12*E*σ12+σ22+σ32-2*ν*(σ1*σ2+σ2*σ3+σ1*σ3)

5.1.1.2 Hydrostatic Loading

Very large amounts of strain energy can be stored in materials without failure if they are hydrostatically loaded to create stresses that are uniform in all directions.

→ This can be done in compression very easily by placing the specimen in a pressure chamber.

→ Many experiments have shown that materials can be hydrostatically stressed to levels well beyond their ultimate strengths in compression without failure, as this just reduces the volume of the specimen without changing its shape.

→ The explanation is that uniform stresses in all directions, while creating volume change and potentially large strain energies, cause no distortion of the part and thus no shear stress.

→ The shear stress is zero, so there is no distortion and no failure. This is true for ductile or brittle materials when the principal stresses are identical in magnitude and sign.

5.1.1.3 Components Of Strain Energy

The total strain energy in a loaded part can be considered to consist of two components- one due to hydrostatic loading which changes its volume, and one due to distortion, which changes its shape.

→ If we separate the two components, the distortion-energy portion will give a measure of the shear stress present.

U=Uh+Ud

Uh=hydrostatic or volumetric component

Ud=distortion-energy component

→ Expressing the principal stresses in terms of hydrostatic and distortion stresses:

σ1=σh+σ1d

σ2=σh+σ2d

σ3=σh+σ3d

→ Adding the three principal stresses:

σ1+σ2+σ3=σh+σ1d+σh+σ2d+σh+σ3d

→ σ1+σ2+σ3=3*σh+(σ1d+σ2d+σ3d)

→ 3*σh=σ1+σ2+σ3-(σ1d+σ2d+σ3d)

→ For Volumetric change with no distortion:

σh=σ1+σ2+σ33

The Strain energy Uh associated with the hydrostatic volume change can be found by replacing each principal stress with σh:

Uh=12*Eσh2+σh2+σh2-2*νσhσh+σhσh+σhσh

Uh=12*E3σh2-2ν3σh2

Uh=321-2νEσh2

Substituting σhinto the equation above

Uh=32(1-2ν)Eσ1+σ2+σ332=1-2ν6Eσ12+σ22+σ32+2(σ1σ2+σ2σ3+σ1σ3)

5.1.1.4 Distortion Energy

The distortion energy Ud is found by adding the total strain energy and the energy due to hydrostatic energy:

Ud=U-Uh=12*E*σ12+σ22+σ32-2*ν*(σ1*σ2+σ2*σ3+σ1*σ3)

-1-2ν6Eσ12+σ22+σ32+2(σ1σ2+σ2σ3+σ1σ3)

Ud=1+ν3*Eσ12+σ22+σ32-σ1σ2-σ2σ3-σ1σ3

For a uniaxial stress state at yield σ1=Sy and σ2=σ3=0:

Ud=1+ν3*E*Sy2

If we take the yielding strength equation above and equate it to the general Ud above, we get:

1+ν3*E*Sy2=Ud=1+ν3*Eσ12+σ22+σ32-σ1σ2-σ2σ3-σ1σ3

→ Sy2=σ12+σ22+σ32-σ1σ2-σ2σ3-σ1σ3

→ Sy=σ12+σ22+σ32-σ1σ2-σ2σ3-σ1σ3 {3D stress state}

For 2D stress state, σ2=0

Sy=σ12-σ1σ3+σ32

→ The two-dimensional distortion-energy equation describes an ellipse, which when plotted on the σ1,σ3 axes. The interior of this ellipse defines the region of combined biaxial stresses safe against yielding under static loading.

5.1.1.5 Von Mises Effective Stress

It is often convenient in situations involving combined tensile and shear stresses acting on the same point to define an effective stress that can be used to represent the stress combination.

Von Mises effective stress σ'

→ is defined as the uniaxial tensile stress that would create the same distortion energy as is created by the actual combination of applied stress.

Von Mises effective stress σ' for the three-dimensional case for three principal stresses:

σ'=σ12+σ22+σ32-σ1σ2-σ2σ3-σ1σ3

Von Mises effective stress σ'for three-dimensional applied stresses:

σ'=(σx-σy)2+(σy-σz)2+(σz-σx)2+6(τxy2+τyz2+τzx2)2

Von Mises for two-dimensional case (with σ2=0):

σ'=σ12-σ1σ3+σ32=σx2+σy2-σxσy+3τxy2

5.1.1.6 Saftey Factor

For design purposes it is convenient to include a chosen safety factor N in the calculation so that the stress state will be safely inside the failure-stress ellipse:

N=Syσ'

For three-dimensional stress case:

SyN=σ12+σ22+σ32-σ1σ2-σ2σ3-σ1σ3

For two-dimensional stress case:

SyN=σ12-σ1σ3+σ32

5.1.1.7 Pure Shear

For the case of pure shear as encountered in pure torsional loading the principal stresses become σ =τ= -σ3 and σ2 =0.

*re-read this section*

5.1.1.8 Ductile Failure Theory

Based on experiments and the distortion energy theory , failure in the case of ductile materials in static tensile loading is considered to be due to shear.

5.1.1.9 A Historical Note

Eichinger (in 1926) and Nadai ( in 1937) independently developed the von mises effective stresses by a different method involving octahedral stresses, and others have arrived at the same result using different approaches.

--> The number of independent developments of this theory using different approaches, in combination with the very close correlation of experimental data to its predictions, make it the best choice for predicting failure in the case of static loading of ductile materials in which the tensile and compressive strengths are equal.

5.1.2 The Maximum Shear Stress Theory

-The maximum shear stress theory was first proposed by Coulomb (1736-1806) and later described by Tresca in an 1864 publication.

-Maximum Shear Stress Theory states that failure occurs when the maximum shear stress in a part exceeds the shear stress in a tensile specimen at yield (one half of the tensile yield strength).

Sys=0.50*Sy

*show figure 5-5*

Figure 5-5 shows the hexagonal failure envelope for the two-dimensional maximum shear theory superposed on the distortion-energy ellipse.

It is inscribed within the ellipse and contacts it at six points.

To use this theory for either two- or three-dimensional static stress in homogeneous,  isotropic,  ductile materials, first compute the three principal stresses σ1, σ2, σ3 ( one of which will be zero for a 2-D case) and the maximum shear stress, τ13.

Then compare the maximum shear stress to the failure criterion in equation 5-10. The safety factor for the maximum shear stress theory is found from:

N=Sysτmax=0.50*Syτmax

Where τmax is the largest result from equation 4.5.

τ13=|σ1-σ3|2

5.1.3 The Maximum Normal Stress Theory

...but it must be noted that it is not a safe theory to use for ductile materials.

--> remember from earlier that most ductile parts will failure due to shear stress. This theory is somewhat useful for brittle materials that have a lower ultimate tensile strength than their shear and compressive strengths.

-failure will occur when the normal stress in the specimen reaches some limit on normal strength such as tensile yield strength or ultimate tensile strength.

5.1.4 Comparison of Experimental Data with Failure Theories

* insert figure 5-8 and insert the corresponding paragraph*

The distortion-energy method is very easy to use, even with only a pocket calculator, and provides a theoretically more accurate result. Nevertheless, since some experimental data fall inside the ellipse but outside the shear hexagon,  some designers prefer the. More conservative approach of the maximum shear theory. As the engineer in charge, the choice is ultimately your decision.

Both the distortion-energy theory and the maximum shear theory are acceptable as failure criteria in the case of static loading of ductile, homogeneous,  isotropic materials whose compressive and tensile strengths are of the same magnitude.

Even Materials- These materials tend to have compressive strengths equal to their tensile strengths, some of these materials are most wrought engineering metals and some polymers.

Uneven Materials- These materials have compressive strengths much greater than their tensile strengths, some of these materials such as cast-brittle metals and composites.

→ These materials require more complex failure theories.

→ Gray cast irons typically have compressive strengths 3 to 4 times their tensile strengths, and ceramics have even larger ratios.

5.2 Failure of Brittle Materials Under Static Loading

Brittle materials fracture rather than yield.

-Brittle fracture in tension- due to normal tensile stress.

→ use maximum normal-stress theory

-Brittle fracture in compression- due to normal compressive normal stress and shear stress.

→ requires a different theory of failure.

5.2.1 Even and Uneven Materials

Another characteristic of brittle materials is that their shear strength can be greater than their tensile strength ( but not greater than their compressive strength).

→ Whereas ductile materials have a shear strength about ½ the tensile strength. Meaning their failure plane is at 45oto the applied tensile stress.

Failure Lines

→ Even Materials, the failure lines are independent of the normal stress and are defined by the maximum shear strength of the material.

→ Uneven materials, the failure lines are a function of both the normal stress σ and the shear stress τ.

For the compressive regime, as the normal compressive stress components becomes increasingly negative (i.e. more compression), the material’s resistance to shear stress increases.

→ More compression makes it more difficult for shear slippage to occur along fault lines within the material’s internal flaws.

5.2.2 The Coulomb-Mohr Theory

→ Coulomb-Mohr Theory for brittle failure.

→ The only differences are the Coulomb Mohr’s asymmetry due to the uneven material properties and its use of ultimate (fracture) strengths instead of yield strengths.

5.2.3 The Modified-Mohr Theory

*It is the preferred failure theory for uneven, brittle materials in static loading.*

If the 2-D principal stresses are ordered σ1>σ3, σ2=0, then only the first and fourth quadrants.

Safety Factor

N=Sutσ1

If the two nonzero principal stresses have opposite sign, then two possibilities exist for failure.

Additional Factor of Safety equation:

N=Sut*|Suc||Suc|σ1-Sut(σ1+σ3)

→ If the stress state is in the fourth quadrant, both safety factor equations should be checked and the smaller resulting safety factor used.

Effective stress that would account for all the applied stresses and allow direct comparison to a material-strength property, as was done for ductile materials with the von Mises stress.

Set of expressions for this effective stress involving the three principal stresses:

C1=12|σ1-σ2|+2*Sut-|Suc|-|Suc|σ1+σ2

C2=12|σ2-σ3|+2*Sut-|Suc|-|Suc|σ2+σ3

C3=12|σ3-σ1|+2*Sut-|Suc|-|Suc|σ3+σ1

The largest of the set of six values (C1, C2, C3, σ1, σ2, σ3) is the desired effective stress as suggested by Dowling.

σ=MAX (C1, C2, C3, σ1, σ2, σ3) 		σ=0  if MAX<0

Modified-Mohr effective stress can now be compared to the ultimate tensile strength of the material to determine a safety factor:

N=Sutσ

5.3 Fracture Mechanics

The static failure theories discussed so far have all assumed that the material is perfectly homogeneous and isotropic, and thus free of any defects such as cracks, voids, or inclusions, which could serve as stress-raisers.

-This is seldom true for real materials.

-Actually, all materials are considered to contain microcracks too small to be seen with the naked eye.

→ …every structure contains small flaws whose size and distribution are dependent upon the material and its processing.

→ These may vary from nonmetallic inclusions and microvoids to weld defects, grinding cracks, quench cracks, surface laps, etc. Scratches or gouges in the surface due to mishandling can also serve as incipient cracks.

→ Functional geometric contours that are designed into the part may raise local stresses in predictable ways and can be taken into account in the stress calculations.

→ Cracks that occur spontaneously in service, due to damage or material flaws, are more difficult to predict and account for.

→ The presence of a sharp crack in a stress field creates stress concentrations that theoretically approach infinity.

kt=1+2ac

Note that when the value of c approaches zero, the stress concentration, and thus the stress, approaches infinity. Since no material can sustain such high stresses, local yielding (for ductile materials), local microfracture (for brittle materials), or local crazing (for polymers) will occur at the crack tip.

→ If stresses are high enough at the tip of a crack of sufficient size, a sudden, “brittle-like” failure can result, even in ductile materials under static loads.

*include figure 4-35 graph

Examples of how fracture mechanics can destroy tankers, pressure vessels, and rocket-motor case.

5.3.1 Fracture-Mechanics Theory

Fracture mechanics presumes the presence of a crack. The stress state in the region of the crack may be one of plane strain or plane stress.

Linear-Elastic Fracture-Mechanics (LEFM)

→ If the zone of yielding around the crack is small compared to the dimensions of the part.

→ LEFM assumes that the bulk of the material is behaving according to Hooke’s law.

→ However, if a significant portion of the bulk material is in the plastic region of its stress-strain behavior, then a more complicated approach is required than that described here.

5.3.1.1 Modes of Crack Displacement

Mode I - the applied loads may tend to pull the crack open in tension.

→ Most of the fracture-mechanics research and testing has been devoted to the tensile loading case.

Mode II - shear the crack in-plane

Mode III - Shear (tear) it out-of-plane

5.3.1.2 Stress Intensity Factor K

The crack is assumed to be sharp at its end, and b is much larger than a. An r-θ polar coodinate system is also set up in the xy plane with its origin at the crack tip. From the theory of linear elasticity, for b>>a the stresses around the crack tip, expressed as a function of the polar coordinates, are

σx=K2πrcosθ21-sinθ2sin3θ2+...

σy=K2πrcosθ21+sinθ2sin3θ2+...

τxy=K2πrsinθ2cosθ2cos3θ2+...

σz=0				→ for plane stress

or

σz=ν*(σx+σy)		→ for plane strain

τyz=τzx=0

Note that, when the radius r is zero, the xy stresses are infinite. The stresses diminish rapidly as r increases.

→ The angle θ defines the geometric distribution of the stresses around the crack tip at any radius.

The high stresses near the crack tip cause local yielding and create a plastic zone of radius ry.

For any radius r and angle θ, the stress state in this plastic zone at the crack tip is directly proportional to the stress intensity factor K.

If b>>a, then K can be defined for the center-cracked plate as

K=σnomπ*a	for a<<b

This equation will be accurate within 10% if a/b ≤0.4.

→ The units of K are either MPa-m0.5 or kpsi-in0.5.

If the crack width a is not small compared to the plate width b, and/or if the geometry of the part is more complicated than the simple cracked plate, then an additional factor β is needed to calculate K.

K=β*σnomπ*a

→ βis a dimensionless quantity that depends on the part’s geometry, the type of loading and the ratio a/b.

→ Values of β for various geometries and loadings can be found in handbooks…

The value of βfor the center-cracked plate can be found

β=secπ*a2*b

This asymptotically approaches 1 for small values of a / b and is ∞ for a / b = 1.

5.3.2 Fracture Toughness K C

Fracture Toughness KC (which is a property of the material) the crack can be considered to be in a stable mode (if the load is static and the environment is non corrosive), in a slow-growth (if the load is time-varying and the environment is non corrosive), or in a fast-growth mode (if the environment is corrosive).

→ However, we will be focusing on stable mode.

When K reaches KC, by reason of an increase in the nominal stress or by growth of the crack width, the crack will propagate suddenly to failure.

→ The rate of this unstable crack propagation can be spectacular, reaching velocities as high as 1 mile/sec!

The factor of safety for fracture-mechanics failure is:

NFM=KCK

Fracture toughness KC for engineering metals ranges from 20 to 200 MPa-m0.5; engineering polymers’ and ceramics’ KC ranges from 1 to 5 MPa-m0.5. Fracture toughness generally parallels ductility and increases substantially at high temperatures.

5.4 Using the Static Loading Failure Theories

The assumed presence of microscopic cracks does not preclude the use of conventional failure theories as long as detectable, macroscopic cracks are not in evidence.

Another fundamental assumption of these static failure theories is that the loads are slowly applied and remain essentially constant with time.

5.4.1 Stress Concentrations

Stress concentrations due to geometric discontinuities or sharp contours needs to be taken into account in some cases of static loading before applying the appropriate failure theory.

under static loading, stress concentration can be ignored if the material is ductile, because the high stress at the discontinuity will cause local yielding that reduces its effect.

for brittle materials under static loading, the effects of stress concentration should be applied to the calculated stresses before converting them to effective stresses for comparison to the failure theories.

5.4.2 Temperature and Moisture

→ Metals typically becomes less strong and more ductile at elevated temperatures.

→ A ductile material can become brittle at low temperatures.

→ Polymers exhibit similar trends over much smaller ranges of temperature than metals.

→ Boiling water is hot enough to soften some polymers, and a cold winter day can make them extremely brittle.

5.4.3 Cracks

→ If macroscopic cracks are present, or are anticipated in service, then the fracture-mechanics (FM) theory should be applied.

→ Once actual cracks are discovered in the field, FM should be used to predict failure and determine the safety of the particular part.

Covered more in depth in the next chapter ( or two).