Chapter 6 - Fatigue Failure Theories

6.0 Introduction

→ Most failures in machinery are due to time-varying loads rather than to static loads.

→ Failures typically occur at stress levels significantly lower than the yield strengths of the materials.

→ These failures typically occur at stress levels significantly lower than the yield strengths of the materials.

6.0.1 History of Fatigue Failure

This phenomenon was first noticed in the 1800s when railroad-car axles began failing after only limited time in service. They were made of ductile steel but exhibited sudden, brittle-like failures.

→ Rankine published a paper in 1843, On the Causes of Unexpected Breakage of Journals of Railway Axles, in which he postulated that the material had “crystallized” and become brittle due to the fluctuating stress.

The mechanism of failure was not yet understood, and the brittle appearance of the failure surface in a ductile material caused speculation that the material had somehow become “tired” and embrittled from the load oscillations.

6.1 Mechanism of Fatigue Failure

Fatigue failures always begin at a crack.

→ The crack may have been present in the material since its manufacture, or it may have developed over time due to cyclic straining around stress concentrations.

→ Fatigue cracks generally start at a notch or other stress concentration.

→ ...the general term notch to represent any geometric contour that increases local stresses.

→ The brittle failures of some of the World War II tankers were traced to cracks that began at an arc-strike left by a careless welder.

→ The Comet airplane failures started at cracks smaller than 0.07 in long crack near the corners of windows that were nearly square, thus providing high stress concentrations.

→ Thus it is critical that dynamically loaded parts be designed to minimize stress concentrations.

There are three stages of fatigue failure:

Crack Initiation- The first stage can be of short duration.

Crack Propagation- The second stage involves most of the life of the part.

Sudden Fracture due to unstable crack growth- The third stage is instantaneous

6.1.1 Crack Initiation Stage

Assume that the material is a ductile metal and as manufactured has no crack present but has the usual collection of particles, inclusions, ect., that are common to engineering materials.

At a microscopic scale, metals are not homogeneous and isotropic. Assume further that there are some regions of geometric stress concentration (notches) in locations of significant time-varying stress that contains a tensile (positive) component.

→ As the stresses at the notch oscillate, local yielding may occur due to the stress concentration, even though the nominal stress in the section is well below the yield strength of the material.

→ The localized plastic yielding causes distortion and creates slip bands (regions of intense deformation due to shear motion) along the crystal boundaries of the material.

→ AS the stress cycles, additional slip bands occur and coalesce into microscopic cracks.

→ Preexisting voids or inclusions will serve as stress-raisers to start the crack.

Less ductile materials do not have the same ability to yield as ductile ones and will tend to develop cracks more rapidly.

→ Brittle materials which do not yield may skip this initiation stage and proceed directly to crack propagation at sites of existing voids or inclusions that serve as microcracks.

6.1.2 Crack Propagation Stage

The sharp crack creates stress concentrations larger than those of the original notch, and a plastic zone develops at the crack tip each time a tensile stress opens the crack, blunting its tip and reducing the effective stress concentration. The crack grows a small amount.

-When the stress cycles to a compressive-stress regime, to zero, or to a sufficiently lower tensile stress, the crack closes, the yielding momentarily ceases, and the crack again becomes sharp, but now at its longer dimension.

Simply put:

-Tensile stress elongates the crack normal to the maximum tensile stress. While also blunting the crack tip.

-Compressive stress closes the crack and sharpens the crack tip.

6.1.2.1 Corrosion

If a part containing a crack is in a corrosive environment, the crack will grow under static stress.

While the frequency of stress cycling appears to have no detrimental effects on crack growth in a non corrosive environment, in the presence of corrosive environments it does.

Lower cyclic frequencies allow the environment more time to act on the stressed crack tip while it is held open under tensile stress, and this substantially increases the rate of crack growth per cycle.

6.1.3 Fracture

The crack will continue to grow as long as cyclical tensile stress and/or corrosion factors of sufficient severity are present.

At some point, the crack size becomes large enough to raise the stress intensity factor K at the crack tip to the level of the material’s fracture toughness KC and sudden failure occurs instantaneously on the next tensile stress-cycle.

→ This failure mechanism is the same whether the condition of K=KC was reached by reason of the crack propagating to a sufficient size or by the nominal stress being raised sufficiently.

→ The result is the same: sudden and catastrophic failure with no warning.

The beachmarks are due to a starting and stopping of the crack growth and they surround the origin of the crack, usually at a notch or internal stress-raiser.

→ The brittle-failure zone is the portion that failed suddenly when the crack reached its size limit.

→ The beachmarks can be seen in the crack zones.

6.2 Fatigue-Failure Models

There are three fatigue failure models in current and each has a place and a purpose:

→ Stress-Life (S-N)

→ Oldest of the three models and is the most often used for high-cycle fatigue (HCF) applications where the assembly is expected to last for more than about 103 cycles of stress.

→ Discussed more in section 6.2.2

→ Strain-Life (ε-N)

→ Combinations of fatigue loading and high temperatures are better handled by this method, because the creep effects can be included.

→ Discussed more in section 6.2.3

→ Linear-Elastic Fracture-Mechanics (LEFM)

→ Fracture-mechanics theory provides the best model of the crack propagation stage of the process.

→ Discussed more in section 6.2.4

6.2.1 Fatigue Regimes

Based on the number of stress or strain cycles that the part is expected to undergo two regimes:

→ low-cycle fatigue (LCF)

→ high-cycle fatigue (HCF)

→ There is no sharp dividing line between the two regimes, and different people list different divisions:

→ Dowling defines HCF starting at around 102 to 104 cycles of stress/ strain variation with the number varying with the material.

→ Juvinall and Shigley suggest around 103 cycles

→ Madayag defines 103 to 104 cycles as the cutoff.

→ This text considers N = 103 cycles

6.2.2 The Stress-Life Approach

It works best when the load amplitudes are predictable and consistent over the life of the part.

It is a stress-based model, which seeks to determine a fatigue strength and/or an endurance limit for the material so that the cyclic stresses can be kept below that level and failure avoided for the required number of cycles.

→ The part is then designed based on the material’s fatigue strength (or endurance limit) and a safety factor.

→ This approach attempts to keep local stresses in notches so low that the crack initiation stage never begins.

→ ...especially for low-cycle fatigue (LCF) finite-life situations where the total number of cycles is expected to be less than about 103 and the stresses will be high enough to cause local yielding.

→ On the other hand, with certain materials, the stress-life approach allows the design of parts for infinite life under cyclic loading.

6.2.3 The Strain-Life Approach

A strain-based model gives a reasonably accurate picture of the crack initiation stage.

→ Because the initiation of a crack involves yielding, a stress-based approach cannot adequately model this stage of the process.

→ It can also account for cumulative damage due to variations in the cycle load over the life of the part…

→ This method is most often applied to LCF, finite-life problems when the cyclic stresses are high enough to cause local yielding.

6.2.4 The LEFM Approach

This method is applied to LCF, finite-life problems where the cyclic stresses are known to be high enough to cause the formation of cracks and is most useful in predicting the remaining life of cracked parts in service.

→ It is often used in conjunction with non destructive testing (NDT) in a periodic service-inspection program, especially in the aircraft/aerospace industry.

Its application is fairly straightforward but relies on the accuracy of the expression for the stress intensity geometry factor β and on the estimate of initial crack size a required for the computation.

It gives more accurate results when a detectable and measurable crack already exists.

→ However, you can fictitiously apply a small “undetectable” crack and solve for a finite life.

6.3 Machine-Design Considerations

The large class of rotating machinery (stationary or mobile) is well served by the stress-life (S-N) model because the required lives are usually in the HCF range.

One class of machinery that typically sees low-cycle fatigue (LCF) is that of transportation (service) machinery.

→ The airframe of an airplane, the hull of a ship, and the chassis of a land vehicle see a load-time history that can be quite variable due to storms, gusts/waves, hard landings/dockings, etc. (for the aircraft/ship) and overloads, potholes, etc. (for the land craft).

Even though the number of low-magnitude stress cycles may be potentially large over its potential lifetime, the chance of higher-than-design loads causing local yielding is always present.

→ A series of high-stress cycles, even if less than 103 in number, can cause significant crack growth due to local yielding.

The strain-life model is best at depicting the conditions of crack initiation and provides the most complete theoretical model but is less well suited to the design of parts for HCF.

→ Strain-life model is more complex than is needed, so we will be focusing on stress-life models. The stress-life model is the most appropriate choice for the majority of rotating-machinery design problems due to the need for high-cycle (or infinite) life in most cases.

6.4 Fatigue Loads

Any loads that vary with time can potentially cause fatigue failure.

→ In rotating machinery, the loads tend to be consistent in amplitude over time and repeat with some frequency.

→ In service equipment, the loads tend to be variable in amplitude and frequency over time and sometimes random in nature.

→ we usually depict the function as a sinusoidal or sawtooth wave.

6.4.1 Rotating Machinery Loading

There are generally three types of cyclical stress-time functions:

→ Fully Reversed Stress: which the mean value is zero.

→ Repeated Stress: in which the waveform ranges from zero to a maximum with a mean value equal to the alternating component.

→ Fluctuating Stress: in which all the components values are nonzero.

These waveforms can be characterized by two parameters:

→ maximum and minimum values

maximum: σmax

minimum: σmin

→ mean and alternating components

σmean=σmax+ σmin2						(6.1c)

σamplitude=σmax- σmin2						(6.1b)

Additionally, stress range Δσ

Δσ=σmax-σmin			(6.1a)

→ ratios of these values

Stress ratio: R=σminσmax					(6.1d)

Amplitude ratio: A=σamplitudeσmean				(6.1d)

→ stress is fully reversed: R=-1 and A=∞

→ stress is repeated R=0 and A=1

→ stress is fluctuating R and A are positive and 0≤R≤1

6.4.2 Service Equipment Loading

The best data come from actual measurements made on equipment in service or operated under simulated service conditions.

→ The automotive test vehicles are extensively instrumented with accelerometers, force transducers, strain gages, and other instruments that feed voluminous amounts of data to on-board computers…

→ The aircraft industry also instruments test-aircraft and records in-flight force, acceleration, and strain data.

→ The same is done with ships and offshore oil platforms, etc.

Data such as these are used in computer simulation programs that calculate the cumulative fatigue damage based on either a strain-based model, a fracture-mechanics model, or a combination of both.

The stress-life model is not able to deal as effectively with this type of loading history.

6.5 Measuring Fatigue Failure Criteria

6.5.1 Fully Reversed Stress

This loading situation can be accomplished with the rotating bending, axial fatigue, cantilever bending, or torsional fatigue tests depending on the type of loading desired.

→ The rotating bending test is a fully reversed, stress-based, HCF test that seeks to find the fatigue strength of the material under those conditions.

→ The axial fatigue test can be used to generate similar fully reversed data to that of the rotating -beam test in a given material and it can also be used to do strain-controlled tests.

→ The principal advantage of the axial test is its ability to apply any combination of mean and alternating stresses.

→ The cantilever bending test subjects a nonrotating beam to oscillations in bending stresses.

→ It can provide a mean stress as well as a fully reversed stress.

→ The torsion test alternately twists a bar in opposite directions applying pure shear stresses.

6.5.1.1 Rotating-Beam Test

R.R. Moore rotating-beam test in which a highly polished specimen of about 0.3-in diameter is mounted in a fixture which allows a constant-magnitude, pure bending moment to be applied while the specimen is rotated at 1,725 RPM.

This creates a fully reversed bending stress at any point on the circumference of the specimen. It is run at one particular stress level until it fails, and the number of cycles to failure and the applied stress level is recorded.

→ This test is repeated with multiple specimens of the same material loaded at different stress levels.

→ The collected data are then plotted as normalized failure strength, Sf/Sut against number of cycles, N, (typically on log-log coordinates) to obtain an S-N diagram.

The data show that samples run at higher reversed-stress levels fail after fewer cycles.

→ At lower stress levels, some do not fail at all before their tests are stopped at some number of cycles (107).

→ Some samples may have contained more, or larger, defects to serve as localized stress-raisers.

6.5.1.2 Endurance Limit

Note that the fatigue strength S falls steadily and linearly as a function of N until reaching a knee at about 106 to 107 cycles.

→ This knee defines an endurance limit Se’ for the material, which is a stress level below which it can be cycled infinitely without failure.

→ At the lower bound of the scatter band beyond the knee, an approximate endurance limit can be defined:

for steels:	Se’ = 0.5*Sut 		Sut < 200 ksi		(6.2a)

Many low-strength carbon and alloy steels, some stainless steels, irons, molybdenum alloys, titanium alloys and some polymers exhibit this knee.

→ Other materials, such as aluminum, magnesium, copper, nickel alloys, some stainless steels, and high-strength carbon and alloy steels show S-N curves that continue to fall with increasing N, though the slope may become smaller beyond about 107 cycles.

For applications requiring <106 cycles of operation, a fatigue strength Sf’ (sometimes also called endurance strength) can be defined at any N from these data. The term endurance limit is used to represent the infinite-life strength only for those materials having one (steels yes, aluminum no).

Steels with higher tensile strengths do not exhibit the relationship shown in equation 6.2a. There is a large scatter band but the average behavior is a line of slope 0.5 up to 200 kpsi. Beyond that level the higher strength steels’ endurance limit falls off. The usual approach is to assume that the endurance limit for steels never exceeds 50% of 200 kpsi.

for higher tensile steels: 	Se’~ 100 ksi		Sut≥200 ksi	(6.2b)

An endurance limit exists only in the absence of corrosion.

Materials in corrosive environments have S-N curves that continue to fall with increasing N. Which will be discussed later on.

*insert figure 6-9*

Aluminum Alloys do not have an endurance limit, thus their fatigue strength Sf ’ is usually taken as the average failure stress at N-5E8 cycles or some other value of N.

Figure 6-11 shows the trend of fatigue strengths (at N=5E8) for a number of aluminum alloys of varying static tensile strengths.

→ The fatigue strength tracks the alloy’s static tensile strengths at a ratio of

for aluminum alloys: Sf ' @5*108≃0.4*Sut          Sut<48 kpsi	(6.2c)

up to a plateau at around Sf '=19 kpsi, indicating that aluminum alloys with Sut about 48 kpsi “top out” at 19 kpsi of fatigue strength.

for aluminum alloys: Sf '@5*108≃19 kpsi                Sut≥48 kpsi	(6.2d)

*Insert Figure 6-11*

6.5.1.3 Axial Fatigue Tests

→ The S-N diagram can also be developed for a material by using an axial fatigue test wherein a specimen similar to that shown in Figure 2-1 is loaded cyclically in a servohydraulic test machine.

→ A principal difference versus the rotating-beam test is that the entire cross section is uniformly stressed in axial tension/compression rather than having a linear stress distribution across its diameter that is maximum at the outer fiber and zero at the center.

→ One result is that the fatigue strengths exhibited in the axial tests are typically lower than those seen in the rotating-beam test.

→ The fact that it is difficult to create exact axial loading with no eccentricity may also be a factor in the lower strength values, since eccentric loads will superpose bending moments on the axial loads.

→ If bending is known to be present in addition to the axial loading, then the reduction may be as large as 40%.

→ The fatigue strength is approximately 80% of the material’s static strength at about 103 cycles and about 40% of its static strength beyond 106 cycles

→ which are both 10% lower than the rotating-beam.

*Insert Graph and a Specimen loaded axially*

6.5.1.4 Cantilever Bending Tests

This test is not used as often as the rotating-bending or axial test but is a less expensive alternative to the latter.

*Insert figure thats loaded for cantilever bending tests & scatter data*

6.5.1.5 Torsional Fatigue Tests

Torsional Fatigue Tests are done on a cylindrical specimen subjected to fully reversed, torsional loading.

→ Note the similarity to the distortion-energy ellipse of figures 5-3 and 5-8, which are for static loading failures.

→ Thus the relationship between torsional strength between torsional strength and bending strength in cyclic loading is the same as in the static loading case.

Torsional fatigue strength (or the torsional endurance limit) for a ductile material can then be expected to be about 0.577 (58%) of the bending fatigue strength (or bending endurance limit).

*Insert figure loaded torsionally and scatter data*

6.5.2 Combined Mean and Alternating Stress

The presence of a mean-stress component has a significant effect on failure.

→ When a tensile mean component of stress is added to the alternating component the material fails at lower alternating stresses than it does under fully reversed loading.

The figure below shows the results of tests made on steels at ≈107to 108cycles and aluminum alloys at ≈5x108 cycles for various levels of mean and alternating stresses in combination.

→ The plots are normalized by dividing the alternating stresses σaby the fatigue strength Sf of the material under fully reversed stress (at the same number of cycles) and dividing the mean stress σm by the ultimate tensile strength Sut of the material.

→ A parabola that intercepts 1 on each axis, called the Gerber line, can be fitted to the data with reasonable accuracy.

→ The Gerber line is a measure of the average behavior of these parameters (for ductile materials) and the goodman line is a measure of their minimum behavior.

→ A straight line connecting the fatigue strength (1 on the y axis) with the ultimate strength (1 on the x axis), called the Goodman line, is a reasonable fit to the lower envelope of the data.

→ The Goodman line is often used as a design criterion, since it is safer than the Gerber line.

6.5.3 Fracture-Mechanics Criteria

To develop fatigue strength data in terms of fracture-mechanics theory, a number of specimens of the same material are tested to failure at various levels of cyclic stress range Δσ.

Reversed-stress tests are seldom done for these data, since compressive stress does not promote crack growth.

The applied stresses range from σmin to σmax. A stress intensity factor range ΔKcan be calculated for each fluctuating-stress condition from

ΔK=Kmax-Kmin:            if Kmin<0       then ΔK=Kmax	(6.3a)

Substituting the appropriate equation:

ΔK=βσmaxπa-βσminπa=βπa*(σmax-σmin)		(6.3b)

The log of the rate of crack growth as a function of cycles da/dN is calculated and plotted versus the log of the stress intensity factor range ΔK.

dadN=A*(ΔK)n

Tested a number of steels and developed empirical values for the coefficient A and the exponent n.

There are three regions:

Region I - crack initiation stage

Region II - crack growth stage

Region III - unstable fracture stage

This “threshold stress intensity factor ΔKthhas often been considered analogous to the unnotched fatigue limit Se , since an applied stress intensity factor range ΔKbelow ΔKth does not cause fatigue crack growth.”

Table Paris-Equation Parameters for Various Steels

|  | MKS | units | IPS | units |
| --- | --- | --- | --- | --- |
| Steel | A | n | A | n |
| Ferritic-Pearlitic | 6.90E-12 | 3.00 | 3.60E-10 | 3.00 |
| Martensitic | 1.35E-10 | 2.25 | 6.60E-09 | 2.25 |
| Austentitic-Stainless | 5.60E-12 | 3.25 | 3.00E-10 | 3.25 |

6.5.4 Testing Actual Assemblies

Some industries will take whole assemblies and/or whole products, and put them through static and/or fatigue stress tests to determine whether or not how a system will fail. These can provide invaluable insight on how the system will act when loaded.

→ Airplane companies put cyclic stresses on airplane wings to determine fatigue failure.

-> While car companies will impact test vehicles to determine whether stresses are great enough to cause plastic deformation to the car frames.

6.6 Estimating Fatigue Failure Criteria

The best information on a material’s fatigue strength at some finite life, or its endurance limit at infinite life, comes from the testing of actual or prototype assemblies of the design as described above.

6.6.1 Estimating the Theoretical Fatigue Strength Sf ‘ or Endurance Limit Se ‘

If published data are available for the fatigue strength Sf ‘  or endurance limit Se ‘ of the material, they should be used and the correction factors discussed in the next section then applied to them.

If no fatigue strength data are available, an approximate Sf ‘  or Se ‘  can be crudely estimated from the published ultimate tensile strength of the material.

→ At high tensile strengths, the fatigue strengths tend to “top out”...

Steels: 		Se'≈0.5*Sut                          for Sut<200 kpsi (1,400 MPa)	(6.5a)

Se'≈100 kpsi (700 MPa)   for Sut ≥200 kpsi (1,400 MPa)

Irons: 			Se'≈0.4*Sut                         for Sut <60 kpsi (400 MPa)		(6.5b)

Se' ≈24 kpsi (160 MPa)     for Sut ≥60 kpsi (400 MPa)

Aluminums:		Sf '@ 5 E 8≈0.4*Sut                         for Sut <48 kpsi (300 MPa)	(6.5c)

Sf '@ 5 E 8≈19 kpsi (130 MPa)     for  Sut ≥48 kpsi (300 MPa)

Copper Alloys:	Sf '@ 5 E 8≈0.4*Sut                        for Sut <40 kpsi (280 MPa)	(6.5d)

Sf '@ 5 E 8≈14 kpsi (100 MPa)    for Sut  ≥40 kpsi (280 MPa)

The fatigue strengths or endurance limits obtained from standard fatigue-test specimens or from estimates based on static tests must be modified to account for physical differences between the test specimen and the actual part being designed.

6.6.2 Correction Factors to the Theoretical Fatigue Strength of Endurance Limit

In the case for fatigue failure, there are several factors that can influence the number of cycles as well as the strength of the part such as loading, environmental, size of the component, and accuracy of the component not failing. These are known as Correctional factors and can be applied to the components fatigue and endurance strengths.

Se=Cload*Csize*Csurface*Ctemp*Creliability*Se '

Sf=Cload*Csize*Csurface*Ctemp*Creliability*Sf '					(6.6)

Cload, Correctional factor for the applied load.

Csize, Correctional factor for the size effects.

Csurface, Correctional factor for any surface defects.

Ctemp, Correctional factor for any radical temperature higher than normal temperatures.

Creliability, Correctional factor for accuracy of a part not failing.

Se, Corrected endurance limit for a material that exhibits a knee in its S-N curve.

Sf, Corrected fatigue strength at a particular number of cycles N for a material that does not exhibit a knee.

6.6.2.1 Loading Effects

Since the ratios described above and most published fatigue strength data are for rotating bending tests, a strength-reduction factor for axial loading must be applied.

Bending:            Cload=1

Axial Loading: Cload=0.70						(6.7a)

→ Use the axial factor if axial loads are present, with or without the bending loads.

Note that a torsional fatigue test shows a strength that is 0.577 times the rotating bending stress’

We will generally deal with the pure torsional case (and all other cases as well) by calculating the von Mises effective stress from the applied stresses.

→ This gives an effective alternating tensile-stress value that can be compared directly to a bending-fatigue strength.

→ So, for pure torsion cases, use Cload=1with this method.

→ use von mises for stress and use correctional factor of one.

6.6.2.2 Size Effects

The rotating beam and static test specimens are small (about 0.3 in diameter).

→ If the part is larger than that dimension, a strength-reduction size factor needs to be applied to account for the fact that larger parts fail at lower stresses due to the higher probability of a flaw being present in the larger stressed volume.

for d≤0.3 in (8 mm)        Csize=1

for 0.3 in<d≤10 in :   Csize=0.869*d -0.097			(6.7b)

for 8 mm <d≤250 mm   Csize =1.189*d -0.097

for larger diameters use Csize =0.6

Valid for cylindrical parts only.

For parts of other shapes, Kuguel suggested that equating the non-round part’s cross-sectional area stressed above 95% of its maximum stress with the similarly stressed area of a rotating-beam specimen would provide an equivalent diameter to use in equation 6.7b.

Since the stress is linearly distributed across the diameter d of a beam in rotating bending, the area A95 stressed above 95% of the outer-fiber stress is that which lies between 0.95*d and 1.0*d.

A95=πd 2-(.95*d) 24=0.0766*d 2					(6.7c)

A95= the portion of cross-sectional area of the non-round part that is stressed between 95-100% of the its maximum stress.

The equivalent-diameter rotating-beam specimen for any cross section:

dequiv=A950.0766							(6.7d)

6.6.2.3 Surface Effects

Surface imperfections can cause stress-raisers that could cause need to have a correction coefficient, Csurface, to help with increasing the fatigue strength.

Rougher finishes will lower the fatigue strength by the introduction of stress concentrations and/or by altering the physical properties of the surface layer.

→ A forged surface is both rough and decarburized and the reduced carbo levels weaken the surface where stresses are often the highest.

→ Note that tensile strength is also a factor, since higher-strength materials are more sensitive to the stress concentrations introduced by surface irregularities.

→ Cast irons can be assigned a Csurface=1,since their internal discontinuities dwarf the effects of a rough surface.

Surface coefficient for steels via graph:

Surface finish via graph and Ultimate Tensile Strength (not material dependent):

Shigley and Mischke suggest using an exponential equation of the form:

Csurface≈A*(Sut)b		if Csurface>1.0, set Csurface=1.0	(6.7e)

|  |  | MPa |  | kpsi |
| --- | --- | --- | --- | --- |
| Surface Finish | A | b | A | b |
| Ground | 1.58 | -0.085 | 1.34 | -0.085 |
| Machined or Cold Rolled | 4.51 | -0.265 | 2.7 | -0.265 |
| Hot-Rolled | 57.7 | -0.718 | 14.4 | -0.718 |
| As-Forged | 272 | -0.995 | 39.9 | -0.995 |

6.6.2.4 Temperature Correction Factor, Ctemp

Fatigue tests are most commonly done at room temperature. The fracture toughness decreases at low temperatures and increases at moderately high temperatures (up to about 350o).

But, the endurance-limit knee in the S-N diagram disappears at high temperatures, making the fatigue strength continue to decline with number of cycles, N.

Also, the yield strength declines continuously with temperatures above room ambient and, in some cases, this can cause yielding before fatigue failure.

The strain-life approach can account for the combination of creep and fatigue under high-temperature conditions and should be used in those situations.

For Steels:

for T≤450oC (840oF)                            Ctemp=1

for 450oC <T≤550oC                          Ctemp=1-0.0058*(T-450)	(6.7f)

for 840oF <T≤1,020oF                      Ctemp=1-0.0032*(T-840)

Note that these criteria are based on data for steels and should not be used for other metals such as Al, Mg, and Cu alloys.

6.6.2.5 Reliability Correction Factors Creliability(or Creliab)

Haugen and Wirsching report that the standard deviations of endurance strengths of steels seldom exceed 8% of their mean values.

Note that a 50% reliability has a factor of 1 and the factor reduces as you choose higher reliability.

→ if you wish to have 99.99% probability that your samples meet or exceed the assumed strength, multiply the mean strength value by 0.702.

Reliability Factors for Sd=0.08μ

| Reliability % | Creliab |
| --- | --- |
| 50 | 1.000 |
| 90 | 0.897 |
| 99 | 0.814 |
| 99.9 | 0.753 |
| 99.99 | 0.702 |
| 99.999 | 0.659 |

6.6.2.6 Environment

The environment can have significant effects on fatigue strength as is evidence by the curves for corroded surfaces.

Note that even room air reduces strength compared to vacuum.

→ The higher the relative humidity and temperature, the larger will be the reduction of strength in air.

→ The increased roughness of the corroded surface is thought to be the reason for the loss of strength.

6.6.3 Calculating the Corrected Fatigue Strength Sf or Corrected Endurance Limit Se

6.6.4 Creating Estimated S-N Diagrams

The bandwidth of interest is the HCF regime from 103 to 106 cycles and beyond.

Let material strength at 103 cycles be called Sm:

bending: 	Sm=0.9*Sut

axial loading:	Sm=0.75*Sut					(6.9)

If the material exhibits a knee, then the corrected Se from equation 6.6 is plotted at Ne=106 cycles and a straight line is drawn between Sm and Se. The curve is continued horizontally beyond that point.

If the material does not exhibit a knee, then the corrected Sf from equation 6.6 is plotted at the number of cycles for which it was generated (shown at Nf = 5*108) and a straight line is drawn between Sm and Sf .

This line may be extrapolated beyond that point, but its accuracy is questionable, though probably conservative.

The equation of the line from Sm to Se or Sf can be written as

S(N)=a*Nb									(6.10a)

or 	log S(N)=log(a)+b*log(N)					(6.10b)

S(N) is a fatigue strength

a & b are constants defined by the boundary conditions..

Boundary Conditions:

b=1z*log(SmSe)                   where z=log(N1)-log(N2)

log(a)=log(Sm)-b*log(N1)					(6.10c)

z-factors for equation 6.10c

| N2 | z |
| --- | --- |
| 1.0E6 | -3.000 |
| 5.0E6 | -3.699 |
| 1.0E7 | -4.000 |
| 5.0E7 | -4.699 |
| 1.0E8 | -5.000 |
| 5.0E8 | -5.699 |
| 1.0E9 | -6.000 |
| 5.0E9 | -6.699 |

6.7 Notches and Stress Concentrations

A notch can be a hole, a groove, a fillet, an abrupt change in cross section, or any disruption to the smooth contours of a part.

→ The notches of concern here are those that are deliberately introduced to obtain engineering such as O-ring grooves, fillets on shaft steps, fastener holes, etc.

→ Notches of extremely small radii are poor design practice and, if present, should be treated as cracks and the principles of fracture mechanics used to predict failure.

→ A notch creates a stress concentration that raises the stresses locally and may even cause local yielding.

In the discussion of stress concentration in Chapter 4 and 5 where only static loads were being considered, the effects of stress concentrations were only of concern for brittle materials.

→ It was assumed that ductile materials would yield at the local stress concentration and lower the stress to acceptable levels.

→ With dynamic loads, the situation is different, since ductile materials behaves as if brittle in fatigue failures.

These factors (Kt  for normal stresses and Kts for shear stresses) give an indication of the degree of stress concentration at a notch having a particular contour and are used as a multiplier on the nominal stress present in the cross section containing the notch.

→ Many of these geometric or theoretical stress-concentration factors have been determined for various loadings and part geometries and are published in various references.

→ For dynamic loading, we need to modify the theoretical stress concentration factors based on teh notch sensitivity of the material to obtain a fatigue stress-concentration factor, kf, which can be applied to the nominal dynamic stresses.

6.7.1 Notch Sensitivity

Notch Sensitivity refer to materials that have different sensitivity to stress concentrations.

→ More ductile the material, the less notch sensitive it is.

→ Brittle materials are more notch sensitive.

→ Since ductility and brittleness in metals are roughly related to strength and hardness, low-strength, soft materials tend to be less notch sensitive than high-strength, hard ones.

→ Notch sensitivity is also dependent on the notch radius (which is a measure of notch sharpness).

→ As notch radii approach zero, the notch sensitivity of materials decreases and also approaches zero.

As notch radii → 0, notch sensitivity goes ↓, and stress-concentration goes ↑.

Like a voltage divider circuit, as the resistance decreases, the voltage at A decreases and current in the circuit increases.

Notch Sensitivity Ratio (Peterson)

q=Kf -1Kt -1									(6.11a)

→ K t is the theoretical (static) stress-concentration factor for the particular geometry.

→ Kf  is the fatigue (dynamic) stress-concentration factor.

→ The notch sensitivity q varies between 0 and 1.

Fatigue (dynamic) Stress-Concentration

The nominal dynamic stress for any situation is then increased by the factor Kf for tensile stress (Kfs for shear stress) in the same manner as was done for the static case.

Kf=1+q*(Kt-1)						(6.11b)

σ=Kf*σnominal

τ=Kf*τnominal								(6.12)

Kuhn-Hardrath Formula (using Neuber’s constant, a, and notch radius, r):

q=11+ar									(6.13)

6.8 Residual Stresses

Residual stress refers to stresses that are “built-in” to an unloaded part. Most parts will have some residual stresses from their manufacturing processes.

Any procedure such as forming or heat treatment that creates localized strains above the yield point will leave stresses behind when the strain is removed.

Compressive Residual Stresses

Since residual stresses, whether deliberately introduced or merely left over from manufacturing processes, will influence the mean stress, their effects can be accounted for. [Roark]

→ Properly done, these compressive residual stresses can make significant improvements in fatigue life.

→ There are several methods for introducing compressive residual stresses:

Thermal Treatments

Surface Treatments

Mechanical Prestressing Treatments

→ Most of them create biaxial compressive stresses at the surface, triaxial compressive stresses below the surface and triaxial stresses in the core.

Since the part is in equilibrium, the compressive stresses near the surface have to be balanced by tensile stresses in the core.

If the treatment is overdone, the increased tensile core stresses can cause failure, so a balance must be struck.

The net tensile stresses at notches will be reduced by adding residual compressive stresses in those locations. Since designed notches are usually at the surface, a treatment can be applied to them.

The deliberate introduction of residual compressive stresses is most effective on parts made of high-yield-strength materials.

If the yield strength of the material is low, then the residual stresses may not stay long in the part due to later yielding from high applied stresses in service.

6.8.0.1 Thermal Treatments

Thermal stressing occurs whenever a part is heated and cooled as in hot-forming or in heat treatment. There are two types of heat treatment:

Through Hardening

→ the entire part is heated above the transition temperature then quenched.

→ Causes tensile residual stresses in the surface

Case Hardening

→ A relatively thin surface layer is heated above the transition temperature and quenched or the part is heated to a lower temperature in a special atmosphere that adds hardening elements to the surface.

→ carburizing, nitriding, flame, or induction hardening creates compressive residual stresses in the surface because the volume increasing associated with the material’s phase change is localized near the surface and the unchanged core pulls the case into compression.

6.8.0.2 Surface Treatments

The two most common methods for introducing surface compressive stresses are shot peening and cold forming.

Both involving a tensile yielding of the surface layer to some depth.

Since we are attempting to protect against tensile stresses in fatigue loading, we want to yield the material in tension to develop compressive residual stresses.

This technique of cold working the surface was known to ancient blacksmiths who hammered the surface or carriage-spring when cold as a final step to increase its strength.

Shot Peening

The surface of the part is impacted with a stream of shot (like buckshot) made of steel, chilled cast iron, glass, ceramic, walnut shells, or other material.

→ The harder shot is used on steel parts and the softer shot on soft, non-ferrous metals.

The impacts of the shot dent the surface, yielding the material and creating a dimpled appearance.

The surface is essentially stretched to a larger area, and the underlying material pulls it back to a state of compressive residual stress.

There can also be some cold working of the surface material, which increases its hardness and yield strength.

It is difficult to accurately determine the level of residual stress in a shot-peened part, as it must be destroyed to do so.

→ The peak compressive stress occurs just below the surface and it decays rapidly with depth.

→ Can penetrate up to 1 mm under the surface.

On very large parts, hammer peening, is sometimes done in which a hand-held air hammer is used to impact highly stressed portions of the surface (such as the roots of gear teeth) with a hardened ball.

Laser Peening

→ Recent development that uses a pulsed laser to peen up to 1 m2 of metal per hour.

→ Each shockwave generated in the material by a laser pulse creates residual compressive stress 1-2 mm deep over a 25 mm2 area, deeper than some shot peening techniques and is claimed to extend fatigue life 3 to 5 times longer than conventional shot-peening techniques.

→ Laser peening is slower and more expensive than shot peening and is sometimes used on critical areas such as the leading edges of turbine blades and the roots of gear teeth after conventional shot peening has been done to the entire part.

Cold Forming

→ Can be done to surfaces of revolution and flat surfaces.

→ The high forces cause local yielding under the roller that results in compressive residual stresses at the surface,

6.8.0.3 Mechanical Prestressing

Prestressing refers to the deliberate overloading of the part in the same direction as its service loading, prior to its being placed in service.

The yielding that occurs during prestressing creates beneficial residual stresses.

6.9 Designing For High-Cycle Fatigue

There are four basic categories that can be treated separately, although three of them are just special cases of the fourth, general case.

→ The uniaxial case represents simple loading cases such as pure axial loading or pure bending.

→ The multiaxial case is general and allows applied normal-stress components on all axes in combination with applied shear stresses on any face of the stress cube.

More often there will be some combination of multiaxial stresses on machine parts.

For Category (I), fully reversed uniaxial stresses. We will combine them all into one category by calculating the von Mises effective stress and comparing it with the corrected bending-fatigue strength of the chosen material.

→ ...eliminates the need for considering a pure torsional as a special case.

For Category (II), fluctuating uniaxial stresses. This adds the complication of mean stresses, and we will employ the Modified-Goodman diagram in addition to the (simpler) S-N diagram.

→ use von Mises effective stress to convert pure torsional loading into an equivalent form of tensile stress.

|  | Fully reversed stresses (σm=0) | Fluctuating Stresses (σm≠0) |
| --- | --- | --- |
| Uniaxial Stresses | Category I | Category II |
| Multiaxial Stresses | Category III | Category IV |

6.10 Designing for Fully reversed uniaxial stresses (Category I)

Some common applications of this category are rotating bending of a shaft that supports a static load, or reversed torque on a shaft with large, oscillating inertia loads and a mean torque that is effectively zero compared to those oscillations.

6.10.1 Design steps for fully Reversed Stresses with Uniaxial Loading:

1. Determining the number of cycles of loading N that the part will experience over its expected service life.

2. Determine the amplitude of the applied alternating loads from zero to peak. Note that a static load on a rotating shaft causes alternating stresses.

3. Create a tentative part-geometry design to withstand the applied loads based on good engineering practice.

4. Determine any appropriate geometric stress-concentration factors Kt (or Kts for shear) at notches in your part’s geometry.

5. Choose a tentative material for the part and determine its properties of interest such as Sut , Sy , Se , (or Sf ‘ at the life required), and q, from your own test data, from the literature, or from estimates as described in this chapter.

6. Convert the geometric stress-concentration factors Kt (or Kts for shear) to fatigue-concentration factors K f using the material’s notch sensitivity, q.

7. Calculate the nominal, alternating stress amplitudes σa (or τa if the load is pure shear)at critical locations in the part due to the alternating service loads based on standard stress-analysis techniques (chapter 4) and increase them as necessary with the appropriate fatigue stress-concentration factors.

8. Calculate the principal-stress amplitudes for the critical locations based on their states of applied stress (Chapter 4). Note that these contain the effects of stress concentrations. Calculate the von Mises effective stress for each location of interest.

9. Determine appropriate fatigue strength modification factors for the type of loading, size of part, surface, etc., as described in Section 6.6. Note that the loading factor Cload will differ based on whether there are axial or bending loads.

→ If the loading is pure torsion, then the von Mises effective-stress calculation will convert it to a pseudo-tensile stress and Cload should then be set to 1.

10. Define the corrected fatigue strength Sf at the requisite cycle life N (or the corrected endurance limit Se for infinite life if appropriate) and a “static” strength Sm @ N=103 cycles from equation 6.9.

→ Create an S-N diagram and/or write equation 6.10 for this tentative material choice.

11. Compare the alternating von Mises effective stress at the most highly stressed location with the material’s corrected fatigue strength Sn taken from the S-N curve at the desired number of life cycles N.

12. Calculate a safety factor for the design from the relationship

Nf=Snσ'

→ Sn is the corrected fatigue strength at the required number of cycles of life taken from the S-N curve.

→ σ' is the largest von Mises alternating stress at any location in the part, calculated to include all stress concentration effects.

6.11 Designing for Fluctuating Uniaxial Stresses

Repeating or fluctuating stresses have nonzero mean components and these must be taken into account when determining the safety factor.

The modified-Goodman line, Gerber parabola, Soderberg line, and the yield line plotted on σm-σaaxes.

→ The Gerber parabola best fits the experimental failure data and the modified-Goodman line fits beneath the scatter in the data.

Both of these lines intersect the corrected endurance limit Se or fatigue strength Sf on the σa axis with Sut on the σmaxis.

→ A yield line connecting Sy on both axes is also shown to serve as a limit on the first cycle of stress.

→ If the part yields, it has failed, regardless of its safety in fatigue.

→ The Soderberg line connects Se or Sf to the yield strength Sy and is thus a more conservative failure criterion, but it does eliminate the need to invoke the yield line.

→ Whichever lines are chosen to represent failure, safe combinations of σm and σalie to the left and below their envelope.

Gerber Parabola: 			σa=Se*1-σm2Sut2			(6.15a)

→ Gerber parabola is a good fit to experimental data, making it useful for the analysis of failed parts.

Modified-Goodman line: 		σa=Se*1-σmSut			(6.15b)

→ The modified-Goodman line is a more conservative and commonly used failure criterion when designing parts subjected to mean plus alternating stresses.

Soderberg line:			σa=Se*1-σmSy			(6.15c)

→ Soderberg line is less often used, as it is overly conservative.

6.11.1 Creating the Modified-Goodman Diagram

→ On the mean stress (σm)axis, the yield strength Sy and the ultimate tensile strength Sut of the particular material are defined at points A, E, and F.

→ On the alternating stress (σa) axis, the corrected fatigue strength Sf at some number of cycles (or the corrected endurance limit Se) and the yield strength Sy of the particular material are defined at points C and G.

→ The line CF is the Goodman line and can be extended into the compressive region based on empirical data.

→ it is conventional to draw the more conservative horizontal line CB to represent a failure line in the compressive region.

The line AG defines yielding in compression:

-σmSyc+σaSyc=1							(6.16a)

Line BC defines fatigue failure in combination with compressive mean stress:

σa'=Sf								(6.16b)

Line CF defines fatigue failure in combination with tensile mean stress:

σm'Sut+σa'Sf=1							(6.16c)

Line GE defines yielding in tension:

σm'Sy+σa'Sy=1							(6.16d)

→ In the tensile region, the line GE defines static yielding static yielding and the failure envelope.

→ the lines CD and DE to account for the possibility of either fatigue or yield failure.

→ If the mean component of stress were very large, and the alternating component very small, their combination could define a point in the region DEF that would be safely within the Goodman line but would yield on the first cycle.

→ Any combination of alternating and mean stress that falls within that envelope (shaded area, ABCDEA) will be safe.

→ Any combination that lands on the line and outside the shaded area will result in failure.

6.11.2 Applying Stress-Concentration Effects with Fluctuating Stresses

The alternating component of stress is treated the same way as it was for the case of fully reversed stress.

→ ...the geometric stress-concentration factor Kt is found, the material’s notch sensitivity q is determined, and these are used in equation 6.11b to find a fatigue stress-concentration factor Kf .

→ The local value of σais then found from equation 6.12 for use in the modified-goodman diagram.

The mean component of stress σmis treated differently depending on the ductility or brittleness of the material.

→ if ductile, on the amount of yielding possible at the notch.

→ Dowling suggests one of three approaches based on Juvinall [41] depending on the relationship of the maximum local stresses to the yield strength of the ductile material.

→ If the material is brittle, than the full value of the geometric stress concentration Kt is usually applied to the nominal mean stress σmnominal to obtain the local mean stress σmat the notch using equation 4.31.

A mean stress fatigue-concentration factor Kfm is defined based on the level of local mean stress σmat the stress concentration versus the yield strength.

→ Three possibilities exist based on the relationship between σmaxand the material’s yield strength Sy .

If Kf*|σmaxnominal|<Sy    then:			Kfm=Kf

→ If σmax<Syno yielding occurs and the full value of Kf is used for Kfm .

If Kf*|σmaxnominal|>Sy  then:				Kfm=Sy-Kf*σanominal|σmnominal|

→ local yielding will occurs on the first cycle after which the maximum stress cannot exceed Sy .

If Kf*|σmaxnominal-σminnominal|>2*Sy  then:		Kfm=0

→ if the stress range Δσ exceeds 2*Sy causing reversed yielding. The maximum and minimum stresses now equal ±Syand the mean stress becomes zero, making Kfm=0.

Note that the stress-concentration factors should be applied to the nominal applied stresses, be they normal or shear stresses.

→ use the von Mises components to find the safety factor.

6.11.3 Determining the Safety Factor with Fluctuating Stresses

The safety factor for any fluctuating-stress state depends on the manner in which the mean and alternating components(from von Mises stresses) can vary with respect to one another in service.

Note that Sf will be used in the following expressions to represent either the corrected fatigue strength at some defined number of cycles or the corrected endurance limit, Se .

6.11.3.1 Case 1

The alternating stress will remain essentially constant over the life of the part but the mean stress can increase under service conditions.

→ Failure occurs at point Q and the safety factor is the ratio of the lines YQ/YZ.

→ σm'@Q=1-σa'Sy*Sy

→ Nf=σm'@Qσm'@Z=Syσm'*1-σa'Sy					(6.18a)

→ If σa' were so large and σm' so small that point Q was on line CD instead of DE

6.11.3.2 Case 2

The mean stress will remain essentially constant over the life of the part but the alternating stress can increase under service conditions.

→ Failure occurs at point P and the safety factor is the ratio of the lines XP/XZ.

→ σa'@P=1-σm'Sut*Sf

→ Nf=σa'@Pσa'@P=Sfσa'*1-σm'Sut					(6.18b)

→ If σm' were so large and σa'so small that point P was on line DE instead of CD.

6.11.3.3 Case 3

Both alternating and mean stress components can increase under service conditions but their ratio will remain constant.

→ Failure occurs at point R and the safety factor is the ratio of the lines OR/OZ or by similar triangles, either of the ratios σm'@R/ σm'@Z or σa'@R/ σa'@Z .

For Alternating stresses:

→ σa'@R=1-σm'@RSut*Sf

→ σa'@R=σa'@Zσm'@Z*σm'@R=σa'σm'*σm'@R

For Mean Stresses:

→ σm'@R=Sfσ'aσ'm+SfSut

→ Nf=σ'm@Rσ'm@Z=Sf*Sutσ'a*Sut+σ'm*Sf

→ There is also the possibility that point R may lie on line DE instead of CD.

6.11.3.4 Case 4

Both alternating and mean stress components can increase under service conditions but there is no known relationship between their amounts of increase.

→ the future relationship between the mean and alternating stress components is either random or unknown, the point S on the failure line closest to the stress state at Z can be taken as a conservative estimate of the failure point.

→ σ'm@S=Sut*Sf2-Sf*σ'a+Sut*σ'mSf2+Sut2

→ σ'a@S= -SfSut*σ'm@S+Sf

→ To establish a ratio for the safety factor, swing point S about point Z to be coincident with line OZS’ at point S’.

→ ZS=σ'm-σ'm@S2+σ'a-σ'a@S2

→ OZ=(σ'a)2+(σ'm)2

→ Nf=OZ+ZSOZ

→ There is also the possibility that point S may lie on line DE instead of CD.

Case 4 gives a more conservative safety factor than case 3.

→ The same approach can be used to obtain safety-factor expressions for stress-component combinations in the left half-plane of the modified-Goodman diagram.

6.11.4 Design Steps for Fluctuating Stresses

1. Determine the number of cycles of loading N that the part will experience over its expected service life.

2. Determine the amplitude of the applied alternating loads (mean to peak) and of the mean load. (see ch 3 and equations 6.1)

3. Create a tentative part-geometry design to withstand the applied loads.

4. Determine any geometric stress-concentration factors Kt at notches in the part’s geometry.

5. Convert the geometric stress-concentration factors Kt to fatigue-concentration factors Kf using the material’s q.

6. Calculate the nominal, alternating tensile-stress amplitudes σa at critical locations in the part due to the alternating service loads based on standard stress-analysis techniques (chapter 4) and increase them as necessary with the appropriate fatigue stress-concentration factors from equation 6.11.

→ Calculate the nominal mean stress amplitudes at the same critical locations and increase them as necessary with the appropriate mean fatigue stress-concentration factors Kfm from equation 6.17.

7. Calculate the principal stress and von Mises stress amplitudes for the critical locations based on their states of applied stress (separately for mean and alternating components).

8. Choose a tentative material for the part and determine its properties of interest such as Sut , Sy , Se , ( or the Sf at the life required), and notch sensitivity q.

9. Determine appropriate fatigue strength modification factors for the type of loading, size of part, surface, etc.

→ Note that the loading factor Cload will differ based on whether there are axial or bending loads.

→ If the loading is pure torsion, then the von Mises effective-stress calculation will convert it to a pseudo-tensile stress and Cload should be set to 1.

10. Define the corrected fatigue strength Sf at the requisite cycle life N (or corrected endurance limit Se for infinite life if appropriate).

→ Create a modified-Goodman diagram using the material’s corrected fatigue strength Sf taken from the S-N curve at the desired number of cycles N.

11. Plot the mean and alternating von Mises stresses (for the most highly stressed location) on the modified-Goodman diagram and calculate a safety factor for the design.

12. Given the fact that the material was only tentatively chosen and that the design may not yet be as refined as possible, the result of the first pass through these steps will most likely be a failed design whose safety factor is either too large or too small.

→ Iteration will be required (as it always is) to refine the design.

6.12 Designing For Multiaxial Stresses In Fatigue

It is quite usual in machinery to have combined loads that create simultaneous time-varying biaxial or triaxial stresses at the same point.

→ A common example is a rotating shaft subjected to both a static bending moment and a torque.

→ Because the shaft is turning, the static moment creates fully reversed normal stresses that are maximum at the shaft’s outer fiber, and the torque creates shear stresses that are also maximum at the outer fiber.

6.12.1 Frequency and Phase Relationships

When multiple time-varying loads are present, they may be periodic, random, or some combination of the two.

If periodic, they can be mutually synchronous or asynchronous.

The most-studied cases are those of periodic, synchronous, in-phase loads that cause combined stresses whose principal directions do not change with time.

Referred to as Simple Multi-axial Stresses.

These situations, in which the directions of the principal stresses vary with time or in which stresses are asynchronous or out-of-phase, are called complex multi-axial stress.

→ “Analysis of this situation is, in general, beyond the current state of the technology. The design process must process by very approximate analyses supported by extensive experimental studies simulating the material and geometry as well as the loading.”

6.12.2 Fully Reversed Simple Multi-axial Stresses

For fully reversed, simple multiaxial stresses in ductile materials, the distortion energy theory is applicable if the von Mises stress is calculated for the alternating components:

For triaxial case:

σ'a=σ1a2+σ2a2+σ3a2-σ1a*σ2a-σ2a*σ3a-σ1a*σ3a			(6.19a)

For biaxial case:

σa'=σ1a2-σ1a*σ2a+σ2a2						(6.19b)

Safety Factor, Nf :

Nf=Snσa'									(6.20)

→ Sn=Sf=fatigue strength

→ σa'=von Mises alternating stress

6.12.3 Fluctuating Simple Multiaxial Stresses

6.12.3.1 Sines Method

Sines developed a model for fluctuating simple mutliaxial stresses which creates an equivalent mean stress as well as an equivalent alternating stress from the applied stress components.

For Triaxial Stress State:

σ'a=σxa-σya2+σya-σza2+σza-σxa2+6*τxya2+τyza2+τzxa22

σ'm=σxm+σym+σzm								(6.21a)

For Biaxial Stress State:

σ'a=σxa2+σya2-σxa*σya+3*τxya2

σ'm=σxm+σym								(6.21b)

The applied stress components in equations 6.21 are the local stresses, increased by all applicable stress-concentrations factors.

The two equivalent stresses σ'aand σ'm are then used in a modified-Goodman diagram and the appropriate safety factor calculated from equations 6.18.

While the individual local stresses in equations 6.19 and 6.21 each can be increased by a different stress-concentration factor, there may be some conflicts when the corrected fatigue strength or endurance limit is calculated for a combined stress state.

→ For example, a combination of bending and axial loading would give two choices for the load factors from equations 6.7a and 6.9.

→ Use the axial factor if axial loads are present, with or without bending loads.

6.12.3.2 von Mises Method

It is recommended using the von Mises effective stress (σ') for both alternating and mean components of applied stress in simple multiaxial stress loading.

Appropriate (and possibly different) stress-concentration factors can be applied to the alternating and mean components of the applied stresses as described in section 6.10.

For Tri-axial Stress State:

σ'a=σxa-σya2+σya-σza2+σza-σxa2+6*τxya2+τyza2+τzxa22		(6.22a)

σ'm=σxm-σym2+σym-σzm2+σzm-σxm2+6*τxym2+τyzm2+τzxm22

For Bi-axial Stress State:

σ'a=σxa2+σya2-σxa*σya+3*τxya2					(6.22b)

σ'm=σxm2+σym2-σxm*σym+3*τxym2

These alternating and mean von Mises effective stresses are then used in a modified-Goodman diagram to determine a safety factor using the appropriate version of equations 6.18.

This approach is more conservative than the Sines method and is thus more appropriate for situations involving stress concentrations due to notches.

6.12.4  Complex Multiaxial Stresses

Many specific cases or complex multiaxial stresses have been analyzed but no overall design approach applicable to all situations has yet been developed.

For common biaxial stress case of combined bending and torsion, such as occurs in shafts, several approaches have been proposed. One of these, called SEQA, which is based on the ASME Boiler Code.

SEQA is an equivalent or effective stress( similar in concept to the von Mises effective stress), which combines the effects of normal and shear stresses and the phase relationship between them into an effective-stress value that can be compared to a ductile material’s fatigue and static strengths on a modified-Goodman diagram.

SEQA=σ2*1+34*Q2+1+32*Q2cos(2*φ)+916Q412

σ=bending-stress amplitude including any stress-concentration effects

Q=2*τσ

τ=Torsional-stress amplitude including any stress-concentration effects

φ=phase angle between bending and torsion

The SEQA can be computed for both mean and alternating components of stress.

The variation of the SEQA effective stress, expressed as a ratio to the von Mises stress for the same bending-torsion combination as a function of two variables: the phase angle φ and the ratio τ/σ.

6.13 A General Approach To High-Cycle Fatigue Design

Whether the loading is uniaxial or multiaxial, bending or torsion, or any combination thereof, the safety factor with this approach is found in the same manner, comparing some combination of alternating and mean von Mises stresses to a line defined by the fatigue tensile strength and a static tensile strength of the material.

→ This eliminates the need for computing separate torsional fatigue strengths.

If you accept the approach outlined in the previous section for multiaxial loadings with stress concentrations, namely using the von Mises stress for both mean and alternating stress components, the difference between uniaxial and multiaxial cases disappears.

Thus, the modified-Goodman diagram provides a universal tool to determine a safety factor for any stress problem, whether static, fully reversed fatigue, or fluctuating fatigue.

The recommended general approach to HCF design with uniaxial or synchronous multiaxial stresses is then:

1. Generate a suitable modified-Goodman diagram from tensile strength information for the particular material.

2. Calculate the alternating and mean components of the applied stresses at all points of interest in the part and apply the appropriate stress-concentration factor to each applied stress component.

3. Convert the alternating and mean components of the applied stresses at any point of interest in the loaded part to alternating and mean von Mises effective stresses using equations 6.22.

4.Plot the alternating and mean von Mises stresses on the modified-Goodman diagram and determine the appropriate safety factor from equations 6.18.

As such, the von Mises approach can be used for both ductile and brittle materials in HCF fatigue loading, since the (correct) assumption is that fatigue failures are tensile failures regardless of the ductility or brittleness of the material.